1. Objective

The goal of this project is to develop an additive-manufacturing-relevant processing workflow for safe, bioresorbable ZK60 magnesium-based nanocomposites [1,2] reinforced with boron nitride (BN) nanoparticles (Jia et al., 2023). By optimizing acoustic powder mixing and comparing rapid hot compaction against conventional sintering, this project aims to produce high-strength, corrosion-resistant biodegradable orthopedic implants while building foundational powder-processing knowledge for future magnesium additive manufacturing (AM) techniques.

Project goals to be achieved simultaneously:

- Fabricate ZK60-BN nanocomposites using acoustic mixing and hot compaction based on optimized baseline conditions (e.g., 90g acceleration, 4 min blending, 60% fill level) [13].

- Compare the mechanical, physical, and corrosion performance of fast hot compaction versus conventional hot compaction followed by argon sintering (Abdrabo et al., 2025)

- Determine the optimal BN nanoparticle concentration (0%, 0.5%, 1.0%, 1.5%, 2.0% vol.) that best balances microhardness, density, corrosion resistance, and surface wettability.

- Evaluate powder characteristics generated by acoustic mixing to provide AM-relevant information regarding flowability, packing, and reinforcement distribution without the use of solvents or high-energy ball milling. This will be quantified through apparent density, tap density, angle of repose, and flowability index calculations.

- Test the fabricated nanocomposite samples for mechanical and corrosion performance (in vitro).

- Conduct comprehensive biological and surface-response testing (contact angle, cytotoxicity, cell adhesion) of the optimized nanocomposites through external collaboration (UARK).

Points to be studied:

- The effect of rapid hot compaction versus conventional sintering on the integrity and surface degradation behavior of ZK60-BN nanocomposites.

  - The effect of eliminating long-duration, high-temperature sintering steps on both internal material densification and external surface response (wettability and degradation rate) will be evaluated

  - The samples will be tested by: Archimedes density, Vickers microhardness, compression testing, SEM, EDS, and XRD phase identification contact angle measurements, and ICP-OES to monitor Mg ion release.

  - A Boron-Nitride volume composition of 1.0% will be used.

  - Hypothesis: Rapid hot compaction will achieve densification and mechanical integrity comparable or superior to conventional argon sintering. By eliminating the extended high-temperature holding time (e.g., 6 hours at 500°C), the rapid compaction process will restrict excessive thermal exposure, thereby minimizing grain growth and improving mechanical bonding. Furthermore, this optimized microstructure, combined with the 1.5% BN concentration, will improve surface wettability and stabilize the material's degradation rate compared to the unmodified ZK60 matrix and conventionally sintered counterparts.

- The impact of BN nanoparticle concentration and acoustic mixing on the in vitro corrosion and mechanical behavior of ZK60 Mg alloys, utilizing the fast-hot compaction method.

  - The effects of varying BN volume fractions (0 to 2.0 vol.%) under optimized acoustic mixing conditions will be evaluated to avoid excessive agglomeration and micro-galvanic corrosion, utilizing a Resodyn Acoustic Mixer.

  - The samples will be tested by: immersion testing (mass loss, pH monitoring, hydrogen evolution), potentiodynamic polarization (PDP), electrochemical impedance spectroscopy (EIS), and optical/SEM microstructural investigation; as well as various mechanical tests such as Density, porosity and flowability.

  - Hypothesis: Acoustic mixing will uniformly disperse BN nanoparticles up to an optimal threshold (likely 1.0 or 1.5 vol.%), yielding peak microhardness and corrosion resistance. Exceeding this threshold (e.g., 3.0 vol.%) will overwhelm the acoustic dispersion capabilities, causing localized BN agglomeration that increases material brittleness and accelerates degradation through micro-galvanic corrosion.

- Powder characterization and flowability optimization for future magnesium additive manufacturing.

  - Assessing how acoustic mixing preserves spherical powder morphology and homogeneous nanoparticle distribution, reducing oxidation risks compared to traditional milling.

  - The powders will be tested by: apparent and tap density, angle of repose (flowability test), particle size distribution, and SEM imaging of mixed powders.

  - Hypothesis: Unlike traditional high-energy ball milling, high-frequency acoustic mixing will successfully embed the BN reinforcements while preserving the spherical morphology of the atomized ZK60 powder. This preserved morphology will yield high packing densities and excellent flowability, confirming the acoustic mixing workflow as a viable, solvent-free preparation method for powder-bed fusion additive manufacturing feedstock.

2. Experimental Work:

2.1. Samples Preparation:

2.1.1. Materials:

- Matrix Material: ZK60 Mg alloy atomized powder (approximate composition: 5.5 wt.% Zn, 0.4 wt.% Zr, balance Mg) with a particle size of approximately 50–100 µm.

- Primary Reinforcement: Hexagonal BN nanoparticles with a particle size of approximately 45–80 nm (depending on supplier batch) and a purity of roughly 99.8%.

Phase 1: Primary BN Concentration Study (Acoustic Mixing & Fast Hot Compaction)

This phase relies solely on acoustic mixing and rapid hot compaction without traditional long-duration sintering.

- Compositions: Four different BN concentrations will be prepared to identify the optimal threshold:

  - 0 vol.% BN (ZK60 control)

  - 0.5 vol. % BN

  - 1.0 vol.% BN (comparison baseline from prior rapid hot-compaction studies) (Abdrabo et al., 2025)

  - 1.5 vol.% BN (prior best-supported concentration for hardness response) [13]

  - 2.0 vol.% BN

- Acoustic Mixing: Powders will be blended using a Resodyn Acoustic Mixer at an optimized baseline of 90g acceleration, 4 minutes of blending time, and a 60% container fill level [13].

- Fast Hot Compaction: The mixed powders will be loaded into a compaction die. Compaction will be applied at a temperature of 250°C and a load of 6 tons for 5 minutes (Abdrabo et al., 2025). (Note: Pressure will be consistently reported in MPa alongside load in tons to account for specific die diameters).

Phase 2: Fast Hot Compaction vs. Conventional Sintering:

This phase will evaluate if rapid hot compaction can reduce or replace long sintering steps without sacrificing structural integrity, density, or corrosion resistance.

- Sample Selection: Two compositions from Phase 1 will be selected for this comparative study: the ZK60 control (0 vol.% BN) and the optimal BN concentration identified in Phase 1 (likely 1.0 or 1.5 vol.% BN).

- Fabrication Routes:

  - Fast Route: Acoustic mixing + hot compaction only (parameters from Phase 1).

  - Conventional Route: Acoustic mixing + hot compaction + traditional argon sintering.

- Sintering Conditions: For the conventional route, compacted samples will be sintered in a tube furnace under an argon atmosphere. The process will run at 500°C with a 6-hour holding time and a heating ramp rate of approximately 8.33°C/min.

3. Samples Testing:

Preliminary Design of Experiments (DOE) investigation: As found in the paper “Effect of Mixing Parameters on the Performance of BN-reinforced Magnesium Nanocomposite Biomedical Implants,” Microhardness was highest at an acceleration of 90g, a blending time of 4 minutes, a fill level of 60%, and a BN concentration of 1.5%. This specific combination of variables will be used for sample testing. All Testing conditions will be conducted according to the ISO standard

3.1 Powder Level Characterization (For various BN concentrations)

3.1.1 Apparent Density:

- The significance of this test is to determine how loosely the mixed powder packs naturally.

- The test will be conducted using a Hall Flowmeter apparatus.

- A specific volume of powder will be poured into the funnel featuring a 2.54mm orifice and permitted to flow freely into a calibrate 25 cm3 cup. The apparent density is calculated by dividing the mass of the powder by the 25 cm3 volume.

- ISO standard states “Measurement of the mass of a certain quantity of powder, which in a loose condition exactly fills a cup of known volume. The loose condition is obtained by using, when filling the cup, a funnel placed at a determined distance above the cup. The ratio between the mass and the volume represents the apparent density.”

3.1.2 Flowability (Flow Rate):

- The significance of this test is to quantify the ease with which the powder flows, which is critical for smooth powder-bed spreading in AM.

- The same Hall Flowmeter apparatus from the Apparent Density test will be utilized.

- The flow rate will be determined by timing how long it takes for a standard mass of the powder (typically 50g) to completely pass through the funnel orifice.

- ISO standard states “Measurement of the time required for 50g of a metallic powder to flow through the orifice of a calibrated funnel of standardized dimensions.”

3.1.3 Tap Density:

- The significance of this test is to determine how tightly the powder packs when subjected to vibration or tapping, simulating the settling of powder during AM processing.

- A known mass of powder will be placed into a graduated cylinder.

- The cylinder will be mechanically tapped until volume settling ceases.

- Testing conditions will be held up to the ISO standard.

  - ISO standard states “A specified amount of powder in a container is tapped by means of a tapping apparatus until no further decrease in the volume of the powder takes place. The mass of the powder divided by its volume after the test gives its tap density.”

3.1.4 Skeletal Density:

- The significance of this test is to determine the true density of the individual ZK60 and BN powder particles before they are subjected to any heat or pressure. This measures internal gas porosity by comparing skeletal density to theoretical density, allowing for suitability for AM processes to be determined.

- Testing will be conducted using a Gas Pycnometer.

- Either Helium or Nitrogen gas will be used to measure the skeletal volume using gas displacement principles and the volume-pressure relationship defined by Boyle's Law

- This is in line with the ISO standard method

3.2 Mechanical & Physical Properties:

3.2.1 Density Testing:

- For all fabricated samples; (Phase 1 fast hot-compacted) and (Phase 2 conventionally sintered).

- The significance of this test is to evaluate the porosity and densification achieved by the different fabrication routes.

- Minimum number of readings = 10 for each condition.

- The Archimedes principle will be used to measure the density of the compacts. Relative density will be calculated using theoretical composite density derived from the rule of mixtures.

3.2.2 Porosity Testing:

- For all fabricated samples; (Phase 1 fast hot-compacted) and (Phase 2 conventionally sintered).

- The significance of this test is to quantify the void fraction within the nanocomposites, providing direct insight into the effectiveness of the hot compaction and sintering processes, as well as predicting potential structural weak points.

- Porosity will be evaluated using two complementary methods:

  - Analytical Method: Porosity percentages will be calculated theoretically by comparing the measured Archimedes density against the theoretical density (derived from the rule of mixtures).

  - Microscopic Method: ImageJ software will be utilized to analyze cross-sectional SEM and optical microscope images for 2D porosity estimation and pore feature measurements.

- Minimum number of readings = 10 images per condition will be analyzed to ensure statistical reliability (if feasible).

3.2.3 Hardness Test:

- For all fabricated samples; (Phase 1 fast hot-compacted) and (Phase 2 conventionally sintered).

- The significance of this test is to investigate the effect of the BN concentration and the compaction/sintering routes on the surface hardness.

- The disc specimens are convenient for Vickers microhardness testing.

- Minimum number of readings = 10 for each set.

- The test will be done at load = 1 kgf and dwell time = 15 sec.

3.2.4 Compression Test:

- For all fabricated samples; (Phase 1 fast hot-compacted) and (Phase 2 conventionally sintered).

- The significance of this test is to compare mechanical properties (elastic modulus, yield/ultimate strengths, and fracture behavior) of different treatment conditions with each other as well as results from the literature.

- The testing conditions according to the ASTM E9-09 will be adapted for small-scale testing. Short cylindrical specimens will be machined according to the die constraints.

- The surfaces of machine plates and the polished specimens will be cleaned by acetone prior to testing.

3.3 Microscopic SEM and EDS (Energy Dispersive Spectroscopy) Investigation:

- For all fabricated samples; before corrosion and after corrosion testing.

- The significance of this investigation is to explain and interpret the results obtained from other tests from a material science point of view (e.g., BN distribution, porosity, and post-corrosion byproduct layers).

- The samples will be prepared as following:

  - Mounted in polymeric material then polished with coarse to fine grinding (400-2000 grit) SiC paper.

  - Polished using an imperial cloth pad with silica powder until a mirror surface is obtained.

  - Samples will be etched just before the investigation (using acetic-picral or acetic-glycol etchants).

  - EDS mapping will be utilized to verify the elemental distribution of the BN nanoparticles.

3.3.1 (XRD) X-ray Diffraction Analysis:

- For selected optimized samples; before and after corrosion testing.

- The significance of this test is to analyze the chemical composition and evaluate the phase stability of the BN reinforcements, as well as to identify surface corrosion byproducts (e.g., magnesium oxides/peroxides).

3.4 Corrosion and Electrochemical Performance (in vitro):

3.4.1 Immersion Test (in vitro):

- For all fabricated samples; (Phase 1 fast hot-compacted) and (Phase 2 conventionally sintered).

- The significance of this test is to study the degradation behavior and mass loss of nanocomposites over an extended period.

- ASTM-G31-72 can be used for the immersion test.

- The test will be conducted for intervals of 7 to 16 days.

- Samples will be immersed in Hank's solution or simulated body fluid (SBF). The temperature will be maintained at 37 °C, and pH changes will be monitored. Hydrogen evolution will be recorded if the sample geometry permits (Amin et al., 2025).

3.4.2 (PDP) Potentiodynamic Polarization Test & (EIS) Electrochemical Impedance Spectroscopy (in vitro):

- For all fabricated samples; (Phase 1 fast hot-compacted) and (Phase 2 conventionally sintered).

- The significance of this test is to evaluate the corrosion potential, the corrosion current density, and the corrosion mechanisms/passivating layers for each fabrication technique for better comparison.

- The ASTM G5-94 standard can be used for this test.

- The test will be performed in the same SBF and same conditions as in the immersion test.

- The process parameters such as scanning rate of Tafel curves will be set to 1 mV/s (Amin et al., 2025) (Abdalla et al., 2022).

3.4.3 Biological and Surface-Response Testing (in vitro) - UARK Collaboration:

- For selected optimized samples (ZK60 control, optimized fast-compacted nanocomposite, and optimized conventionally sintered nanocomposite).

- The significance of this test is to verify whether processing improvements that enhance mechanical and corrosion behavior translate into acceptable preliminary cytocompatibility (Jia et al., 2023).

- ISO-10993 standard may be followed.

- The testing will include:

  - Contact Angle: Measurement utilizing DI water and/or SBF to compare surface wettability and hydrophilicity across both fast-compacted and conventionally sintered routes [2,3].

  - Cytotoxicity Test: Extract-based testing using MC3T3-E1 preosteoblast cells to verify cell viability specifically for the ZK60 alloy composite under the newly optimized rapid compaction parameters. [2,3].

  - Cell Adhesion & Morphology: SEM imaging will be used to evaluate how cells attach and spread on the ZK60 versus the BN-reinforced surfaces [2,3].

  - Ion Release: ICP-OES will be used to quantify magnesium ion release into the media to determine the degradation stability of the uniquely processed ZK60 matrix.

References:

- Abdrabo, M., Tanveer, T., McGehee, T., Elsaadany, M., and Ibrahim, H., "Effect of Mixing Parameters on the Performance of BN-reinforced Magnesium Nanocomposite Biomedical Implants," Manuscript draft.

- Jia, M. S., Hash, S., Reynoso, W., Elsaadany, M., and Ibrahim, H., 2023, "Characterization and Biocompatibility Assessment of Boron Nitride Magnesium Nanocomposites for Orthopedic Applications," Bioengineering, 10(7), p. 757.

- Amin, A., McGehee, T., Williams, B., Navarro, A., Elsaadany, M., and Ibrahim, H., 2025, "In Vitro Assessment of Magnesium-Based Hybrid Nanocomposites for Bone Implant Applications," Proceedings of the ASME 2025 International Mechanical Engineering Congress and Exposition (IMECE), Memphis, TN, Paper No. IMECE2025-166907.

- Abdrabo, M., Tanveer, T., Patel, D., and Ibrahim, H., 2025, "Fabrication and Characterization of High-Strength Magnesium-Based Nanocomposite Orthopedic Implants by Optimizing Compaction Parameters," Proceedings of the ASME 2025 International Mechanical Engineering Congress and Exposition (IMECE), Memphis, TN, Paper No. IMECE2025-166905.

- Ibrahim, H., Esfahani, S. N., Poorganji, B., Dean, D., and Elahinia, M., 2017, "Resorbable Bone Fixation Alloys, Forming, and Post-Fabrication Treatments," Materials Science and Engineering: C, 70, pp. 870-888.

- Abdalla, M., Sims, A., Mehanny, S., Haghshenas, M., Gupta, M., and Ibrahim, H., 2022, "In Vitro Electrochemical Corrosion Assessment of Magnesium Nanocomposites Reinforced with Samarium(III) Oxide and Silicon Dioxide Nanoparticles," Journal of Composites Science, 6(6), p. 154.

- Heaney, D. F., 2019, "Powders for Metal Injection Molding (MIM)," Handbook of Metal Injection Molding, 2nd ed., D. F. Heaney, ed., Woodhead Publishing, Cambridge, UK, pp. 50.

- Safariland, "Safety Data Sheet: Magnesium Powder," accessed June 23, 2026, https://sds.chemtel.net/webclients/safariland/raw_materials/Magnesium%20Powder.pdf.

- Materials Research Institute, "Density / Helium Pycnometry," The Pennsylvania State University, accessed June 23, 2026, https://www.mri.psu.edu/materials-characterization-lab/characterization-techniques/density-helium-pycnometry.x

Vendors for Magnesium:

- https://heegermaterials.com/spherical-powder/1885-magnesium-alloy-atomized-spherical-powder.html

- https://www.attelements.com/additive-manufacturing-3d-printing-materials/magnesium-alloy-zk60-atomized-spherical-powder.html

- https://nanochicago.us/shop/microparticles/alloy-micron-powder/zk60-magnesium-alloy-micron-powder-size-range-20-63-µm-spherical/

- https://shop.nanografi.com/newly-released-products/zk60-magnesium-alloy-micron-powder-size-range-20-63-m-spherical/

- https://powdernano.com/product/zk60-magnesium-alloy-micron-powder-zk60-mg-20-63-µm-spherical/

Equipment Vendors:

- Gas Pycnometer for Skeletal Density testing: https://www.malvernpanalytical.com/en/products/product-range/accupyc?utm_source=google&utm_medium=cpc&utm_campaign=EN%20-%20Search%20-%20Micromeritics%20-%20NORAM&utm_term=pycnometer&utm_content=EN%20-%20Product%20Category%20-%20Gas%20Pycnometer&gad_source=1&gad_campaignid=22332900911&gbraid=0AAAAAD4oRF3w4z24tyfmcO0mGaxmeI8d3&gclid=EAIaIQobChMI0ZTX8cKdlQMVGbIDAB2eChHlEAAYASAAEgJfbvD_BwE

https://www.ami-instruments.com/product/densi-100/